## Slide 1: Figures

## Slide 2
SMILES
*CC(c1ccccc1)*
Feature generation
Chemical descriptors
Regressor
Labelled data
Predictions
Un-labelled data
Contextual features
Embeddings
Multi head attention
layer
Add & Norm.
FCNN
Add & Norm.
Encoder
Fig1

## Slide 3
Fig1
Labelled data
Contextual features
Regressor
Predictions
Un-labelled data
Embeddings
Multi head attention
layer
Add & Norm.
FCNN
Add & Norm.
Encoder
GPR
SMILES
*CC(c1ccccc1)*
Feature generation
Chemical descriptors
Predictions

## Slide 4: Datasets
Dataset | Property | No.of data points | C.V folds
Eea | Electron affinity | 368 | 5
Egb | Bandgap(Bulk) | 561 | 5
Egc | Bandgap(chain) | 3380 | 5
Ei | Ionization energy | 370 | 5
Xc | Crystallisation tendency | 432 | 5
OPV | Power conversion efficiency | 1203 | 5
EPS | Dielectric constant | 382 | 5
Nc | Refractive index | 382 | 5
LiC | Conductivity | 271 | 5
Eatm | Atomization energy | 351 | On test data
Table1

## Slide 5
PROPERTY | RMcSE |  |  |  |  | R2 score |  |  |  | 
 | Chem | Transpolymer | TransChem | MT | MT+Chem | Chem | Transpolymer | TransChem | MT | MT+chem
Eea | 0.393 | 0.315 | 0.297 | 0.300 | 0.294 | 0.86 | 0.91 | 0.920 | 0.922 | 0.925
Egb | 0.601 | 0.52 | 0.501 | 0.467 | 0.508 | 0.903 | 0.93 | 0.933 | 0.942 | 0.9309
Egc | 0.63 | 0.45 | 0.44 | 0.508 | 0.510 | 0.834 | 0.92 | 0.920 | 0.888 | 0.891
EI | 0.452 | 0.39 | 0.377 | 0.399 | 0.373 | 0.785 | 0.84 | 0.841 | 0.823 | 0.837
Xc | 17.010 | 16.57 | 16.203 |  |  | 0.483 | 0.50 | 0.521 |  | 
OPV | 2.141 | 1.92 | 1.775 |  |  | 0.161 | 0.32 | 0.423 |  | 
EPS | 0.551 | 0.52 | 0.512 | 0.541 | 0.543 | 0.744 | 0.76 | 0.778 | 0.750 | 0.754
Nc | 0.138 | 0.1 | 0.089 | 0.097 | 0.095 | 0.70 | 0.82 | 0.830 | 0.824 | 0.835
LiC | 0.721 | 0.827 | 0.685 |  |  | 0.573 | 0.327 | 0.623 |  | 
Eatm | 0.0392 | 0.053 | 0.034 |  |  | 0.98 | 0.97 | 0.989 |  | 
Table2

## Slide 6
Parity plots
Parity plots
Fig2
b)
c)
a)
d)

## Slide 7
b)
a)
c)
d)

## Slide 8
Fig3
Eatm
Nc
b)
c)
a)
d)

## Slide 9
Egb | 450
Eea : | 4013
EI | 3990
Egc | 2705
Xc | 9070
OPV | 4810
EPS | 4180
Nc | 307
LiC | 12757
Eatm | 4381